FIGURE 3:  2-HOUR FIRE-RESISTANCE RATED EXTERIOR WALL ASSEMBLY

Use where wall is required to be rated from the exterior and interior sides.

INTERIOR SIDE: Base layer 5/8 inch (15.88 mm) type X gypsum wallboard applied parallel to studs with 6d coated nails, 1-7/8 inch (228.6 mm) long, 0.0915 inch (2.48 mm) shank, ¼ inch (6.35 mm) heads, 12 inches (304.8 mm)  o.c. Face layer 5/8 inch (15.88 mm) type X gypsum wallboard applied at right angles to studs with 8d coated nails, 2-3/8 inch long, 0.113 inch (2.87 mm) shank, 9/32 inch (7.14 mm)   heads, 8 inches (203.2 mm)  o.c. at edges and 12 inches (304.8 mm)  o.c. at intermediate studs. (LOAD-BEARING, 100% of Calculated Design Load)

STUD CAVITY: Spaces between the studs are completely filled with rockwool or slag mineral wool batts weighing not less \		        than 3.3 pounds per cubic foot (1 pound per square foot of wall surface).

EXTERIOR SIDE: Pyro-Guard Treated Plywood fastened at 6 inches (152.4 mm) on center at edges and 12 inches (304.8   		           mm) on center in the field covered with a water resistive barrier.

EXTERIOR FINISH: Minimum ¾ inch stucco installed and reinforced per manufacturer instructions, minimum ¾-inch 				 thick full course brick or stone finish, combination of minimum ½-inch noncombustible veneer 				 (stone, brick, tile etc) with a minimum ½-inch backer unit.